## Slide 1: Fatigue and Dwell Fatigue studies on Ti-6242 and Ti-6246 Alloys
Presented by
Sharan Chandran
Under the guidance of
Prof. Dipankar Banerjee and Prof. Satyam Suwas
Department of Materials Engineering

## Slide 2: Outline
Literature review
      Introduction to titanium alloys
      Introduction to Dwell Fatigue
      Phenomenological aspects of Dwell Fatigue
Motivation and objective
Current work
      Modelling
      Experiments
Summary and future work

## Slide 3: Introduction to Titanium Alloys
Alpha | Alpha + Beta | Beta

## Slide 4: What is Dwell Fatigue ?
Fig 1. Schematic of a typical flight cycle
M.R. Bache, International Journal of Fatigue, 2003
Ref: Wikipedia
Ref: Wikipedia

## Slide 5
DFD =
=1 Dwell Insensitive
>10 Highly Sensitive
Accelerated tests are not possible
even though there is no corrosion
or heat generation issue.
But there is creep issue
TIMETAL 685, 20°C
TIMETAL 834, 20°C
Fig: DFD in two Ti alloys
W.J.Evans, 1998
Fig: DFD in two Ti alloys
W.J.Evans, 2001
Why near alpha ?? In these applctins
Dwell Fatigue Debit

## Slide 6
Fig: Perspectives on Titanium Science and Technology, D. Banerjee, et.al., 2014

## Slide 7: Dwell Fatigue Testing
Surface is not very critical
in the case of dwell fatigue
as it is close to low cycle
fatigue
Instron fatigue testing machine
100kN, Servo-hydraulic
Vacuum Sealed and Heat treated to the desired condition
Load Controlled Dwell Fatigue
test at RT
Load for 0.95 proof
Load
120 sec
1s
1s
Time
1s
Normal fatigue
Dwell fatigue
6mm